IC-710

Internal Pipe Coat

Description

IC-710 is an environmentally friendly mineral oil combined with a complex corrosion inhibitor system.  It is designed for protection of oilfield pipe.  It will not dry out, gum up or reduce the internal diameter of the pipe.  The slightly tacky film will provide long term protection to the I.D. and can also be used externally for short term protection.

Application

IC-710 may be sprayed, brushed or dipped.  Use on tubular goods for I.D. or O.D. corrosion protection.  It is best sprayed by compressed air sprayer or airless pump.

IC-710 is to be applied as is.  No special disposal or handling is required

Features

INTERNAL CORROSION PROTECTION

WILL NOT DRY OR GUM UP

ENVIRONMENTALLY FRIENDLY

COATING MAY BE SPRAYED, BRUSHED OR DIPPED

IC-710

Methods of Application

COMPRESSED AIR SPRAYER

AIRLESS PUMP

APPLY AS IS

Physical Properties

Appearance				Light Yellow Liquid

Pour Point				NA

Flash Point, COC			300° F

pH, 1% Solution			NA

Specific Gravity, 72°			0.91

Density, Lbs./Gal. 72° F		7.58

Viscosity, 72° F			80-100 CPS

Solubility, 10%

Water				None

Isopropanol			None

Kerosene			Yes

Xylene				Yes

Titan Chemical Corp.

6710 Cadillac St.

Houston, Texas 77021

713-747-3134