## Slide 1: On-Line Analysis and control of Shredded Aluminum
Using gamma-tech cb-rm analyzer

## Slide 2
Value of The Analyzer in The Aluminum Industry
The Value
The value of knowing what we are buying &melting – removing the hidden costs
The value as process control instrument to provide means to change the scrap product

## Slide 3
UBCs
Class
Shred
Home
RSI
Prime
Product Chemistry
Hidden Variability
Problems
Product Chemistry
Charge Optimization
Known Analysis
The Value of Knowing
Removing the unknown

## Slide 4
Shredder Before Analyzer
Shredder After Analyzer
Charge Optimization
Product Chemistry
The Value of Improved Process Control
Changing The Scrap Product

## Slide 5
UBCs
Class
GammaShred
Home
RSI
Prime
Charge Optimization
The Value of Analyzed Shredded
Lower Raw Material Cost
Environmental Impact - Lower CO2
Increase Productivity
Diluents
Analyzer Installed where Scrap is Processed
The Value - Minimize Diluents

## Slide 6: Analyzer performance for selected elements
CB-RM Results vs. Furnace
9 - 40,000 lb. loads.
August 2019 – July 2020
Element | Accuracy† | Range
Si | ±0.05% | 0.44 - 0.65%
Fe | ±0.03% | 0.31 - 0.46%
Cu | ±0.02% | 0.09 - 0.23%
Cr | ±0.01% | 0.02 - 0.05%
Mn | ±0.01% | 0.23 - 0.43%
Zn | ±0.07% | 0.10 - 0.27%
† RMSD, 1-hour sample period

## Slide 7: accuracy plots
Chart: Si
| 0.58499999999999996 | 0.66500000000000004 | 0.63500000000000001 | 0.45499999999999996 | 0.45 | 0.62249999999999994 | 0.46249999999999997 | 0.57250000000000001 | 0.35249999999999998
Lab | 0.59 | 0.63 | 0.65 | 0.47 | 0.48 | 0.5 | 0.48 | 0.59 | 0.44
 | 0 | 1
Chart: Fe
| 0.39750000000000002 | 0.39750000000000002 | 0.40750000000000003 | 0.46750000000000003 | 0.43 | 0.42499999999999999 | 0.39500000000000002 | 0.39500000000000002 | 0.29500000000000004
Lab | 0.43 | 0.41 | 0.37 | 0.46 | 0.38 | 0.39 | 0.41 | 0.4 | 0.31
 | 0 | 0.8
Chart: Cu
| 0.1825 | 0.2225 | 0.21249999999999999 | 0.1925 | 0.18 | 0.20750000000000002 | 0.19750000000000001 | 0.16749999999999998 | 0.13750000000000001
Lab | 0.19 | 0.23 | 0.22 | 0.17 | 0.16 | 0.21 | 0.21 | 0.2 | 0.09
 | 0 | 0.4
Chart: Mn
| 0.32750000000000001 | 0.28750000000000003 | 0.26750000000000002 | 0.4375 | 0.3 | 0.38728385615914301 | 0.37361897475133887 | 0.31895944912012242 | 0.23013771996939555
Lab | 0.32 | 0.29 | 0.28 | 0.43 | 0.29 | 0.39 | 0.37 | 0.32 | 0.23
 | 0 | 0.8

## Slide 8: Production
Chart: Shredded Aluminum Control
Daily production run
Controlled for Si and Cu limits
Analysis allows for control
Handling and shipping mixes material
Final chemistry meets spec

## Slide 9: Value
Furnace has experienced no out of spec shipments in more than 1 year.
More than 100 million pounds of analyzed shred has been melted.
Allows for increase in shred usage and decrease of prime grades and RSI.
Shredders ability to analyze and blend increases availability of shred.
Shredder reduces/eliminates downgrades.
Can blend from more sources to increase to production.
Improves quality
Improved quality translates to increase in demand (in this case shredder has increased shipments by 23%).
For the Shred Consumer:
For the Shred Processor:

## Slide 10: Where we are going
Features:
Isotope OR Neutron Generator for excitation
Modular design
Variable tunnel height based on process
State-of-the-art electronics

## Slide 11: Process and raw materials optimization
Sorter
Out of Spec
Analyzed
Raw Materials
RSI
Prime
other
Inbound Shred
Furnace
Raw Materials Inventory
Charge Blending
In Spec
Re-analyze
CB-RM Analyzer