HDS Plus

Product data

This product is a combination of selected surfactants, penetrants and fast acting oil emulsifiers.  It easily penetrates, absorbs, and emulsifies to float away grease and oil but leaves no greasy film or residue. HDS Plus is not harmful to aluminum and other soft metals when used in dilution.  This product is recommended for cleaning and degreasing of aircraft, tank cars and trucks.

Typical Properties

Appearance				Purple, Sassafras Odor

Pour Point				20 Degrees

Flash Point				None

pH (1% Solution)			11.0-11.5

Specific Gravity, 72 Degrees F	1.129

Density, Lbs./Gal. 72 Degrees F	9.1

Viscosity, 72 Degrees F		15-20 cps

Solubility 				10 %

Water					Complete

Isopropanol				Dispersible

Kerosene				No

Xylene				            No

Heavy Aromatic Naptha	 	No

Acid No. (MG.KOH/G)

pH 5.5					N/A

pH 9.5					N/A

Application

May be sprayed, mopped or wiped on.  If used through pressure washer or

steam cleaner, dilute with water.  Dilute up to 30-1 with water.

6710 Cadillac Street, Houston, Texas 77021