TC-777

product data

A series of phosphate esters supplied as the free acid with moderate to high foaming properties.  Neutralization with an alkyl or alkanolamine will alter its’ solubility.  Generally these products have excellent coupling properties and high electrolyte tolerances.

Typical Properties

Appearance			Clear Amber

Liquid Pour Point		<40 F

Flash Point, TCC F		>200 F

pH, (1% solution)		1.5-2.5

Specific Gravity		1.16

Density, Lbs/Gal 72 F		9.7

Viscosity, 72 F

Solubility, 10%

Water			Soluble

Isopropanol		Soluble	Kerosene		Insoluble	Caustic Soda 50%	>30%

Acid No. (MG. KOH/G)

pH 5.5			145-180	pH 9.5			280-320

Application

The outstanding oil and grease removal characteristics of these compounds make them excellent candidates for use in highly alkaline cleaner, liquid or dry blended.