Product Bulletin

Coat 200

Low VOC Waterbased Pipe Coating

Description

Coat -200 is designed as a waterbased air-dry industrial coating. The balance of properties offered by Coat -200 provides fast dry, excellent rust protection and a high gloss finish for pipe during outdoor storage.  Coat -200 is waterbased, contains no Hazardous Air Pollutants and low Volatile Organic Compounds.

Usage

The corrosion of pipe or equipment during storage usually causes more damage and metal loss than during actual use.  The use of Coat -200 protects metallic surfaces from the damaging effect of high humidity and high salt concentrations.  When   applied to clean dry pipe or metal, it produces a tough, transparent film.

Features

Low VOC

Fast Air Dry

Early Water Resistance

Resistance To Salt and Humidity

Excellent Gloss

Exceptional Adhesion

non- flammable

Clean-up with soap and water

Application

Coat -200 can be applied on ferrous and  nonferrous metal piping.  Surface preparation should include pipe that is clean and dry.  Coat -200 should be applied when ambient and surface temperature is 40˚ F or above when possible.  Methods of application include airless and conventional sprays, Nordson spray systems, and dip and flow coater. Periodic agitation of product is recommended.

COAT -200

Physical Properties

Type						Acrylic polymer

Solids				                        Approx. 25%

Weight Per Gallon				8.43 +/-0.2 lb. per gallon

Viscosity   Krebs Units		            50-60 KUs

#4 Zahn Cup                                 18-24 seconds.

Blue Cup				17-19 seconds.

Color	                                                            Transparent / black

pH						8.30-8.80

Flash Point-COC				None

Dry to touch @77°/25°C		            < 5 Minutes

Curing Time @77°/25°C			< 2 Hours

VOC:					            0.46 Lbs. /Gallon

Typical coverage	                                    401 – 601 ft² / gal

Wet film thickness                                          4-6 mil.

Dry film thickness                                          1.00-1.50 mil

Titan Chemical Corporation

6710 Cadillac St.

Houston, Texas 77021

713-747-3134