A close up of a logo

AI-generated content may be incorrect.

|  |  |  |
| --- | --- | --- |
| **Elastomer Family** | **ASTM** | **Shelf Life** |
| Aflas |  | Unlimited |
| Butyl Rubber, lsobutylene lsoprene | llR | Unlimited |
| Chloroprene (Neoprene®) | CR | 15 Years |
| Epichlorohydrin (Hydrin®) | ECO | N/A |
| Ethylene Acrylic (Vamac®) | AEM | 15 YEARS |
| Ethylene Propylene, EPDM or EP | EP | Unlimited |
| Fluorocarbon (Viton®) | FKM | Unlimited |
| Fluorosilicone | FVMO | Unlimited |
| Hydrogenated Nitrile, HNBR or HSN | HNBR | 15 YEARS |
| Nitrile (Buna-N or NBR) | NBR | 15 YEARS |
| Perfluorelastomer | FFKM | Unlimited |
| Polytetrafluoroethylene (Teflon®) | PTFE | N/A |
| Polyacrylate | ACM | 15 YEARS |
| Polyurethane (Polyester or Polyether) | AU / EU | 5 Years |
| Silicone | VMO | Unlimited |
| Styrene Butadiene (Buna-S) | SBR | 3 YEARS |

A blue and black text

AI-generated content may be incorrect.Seal-Jet of Ohio, Inc accepts no responsibility for results obtained. Each user of these products, or information, should perform their own tests to determine the suitability of the material. Seal-Jet does not guarantee that the user will obtain the same results. The data and information are subject to change without notice.