ABCO PCS

ABCO Products of Sacramento

Primary Usage

ABCO PCS is a surface stripping formulation for the Powder Coating Industry, which provides a high degree of efficiency without sacrificing safety and protection of the environment.

# Application

ABCO PCS is used concentrated.

- Temperature	130F – 150F  (do not exceed 150F)

- Time		Varies, depending on thickness and type of coating.

- Agitation 		Mechanical agitation is recommended

- Keep covered at all times to avoid evaporation.

# Chemical Composition

Ethanolamine

# Performance Data

This product is designed to perform on polyurethane’s, epoxies, polyamides and a variety of surface coatings, without harming the base aluminum, titanium, stainless steel, and high-strength steels.

Floating seal high-flash mineral oil based minimizes drag out, odor and evaporation.

## Equipment, Tanks and Heaters - Steel or stainless steel.

Caution: Wear protective equipment when handling

8290 Alpine Avenue · Sacramento, CA 95826 · Ph: (916) 447-9931 · Fax: (916) 443-7466