ABCO Soak Cleaner 922

ABCO Products of Sacramento

Primary Usage

ABCO Soak Cleaner 922 is designed for use where extremely adverse cleaning conditions exist. It is an extra heavy-duty material giving fast soil removal, excellent rinsability and long bath life.

# Application

Use ABCO 922, 6 to 12 ounces per gallon of water, at temperatures of 150 to 180F. Immersion time from 5 to 20 minutes. Follow with good rinsing practices. Concentrations, temperatures and immersion time will vary with condition of the parts.

# Chemical Composition

Alkaline cleaning compound

# Performance Data

ABCO 922 may be effectively used as a pre-soak cleaner prior to electro plating as a hot tank cleaner in a phosphate line, and for cleaning prior to porcelain enameling. Soak cleaner 922 is also used for barrel cleaning prior to zinc and cadmium plating.

# Analytical Procedure

- Pipette a 5.0 ml sample into a 250 ml beaker

- Add 50-75 ml distilled water and 3 drops of phenolphthalein indicator

- Titrate with 1.0 N Hci until pink color disappears completely

- Calculation: oz/gal Soak Cleaner 922 + ( ml 1.0 N Hcl ) ( 1.584 )

# Caution: ABCO Soak Cleaner 922 is a alkaline and can cause burns. Exercise caution in its use. Wear protective equipment when handling.

8290 Alpine Avenue, Sacramento,  CA  95826            Ph:  ( 916) 447-9931         Fax:  (916) 443-7466