## Slide 1
Over-view of
Iron & Steel Making
Mr. Bhavesh C. Lad
Sr. Manager, Technology Group
THEIS PRECISION STEEL INDIA PVT. LTD

## Slide 2: Contents
History of iron making
Flow diagram of iron making to steel making
Different Section of Iron making
Basics of Blast Furnace (Introduction to blast furnace)
History of Steel Making
Introduction of Steel Making Furnaces
Ladle treatment / degassing treatment
Continuous casting process
Hot rolling

## Slide 3: 1. 3500BC Beads in Ancient Egypt for iron. 2. First Iron Production 3000BC Syria and Mesopotamia the comparatively advanced technique of hardening iron weapons by heat treatment was known to the Greeks about 1000 BC. 3. They were made by heating a mass of iron ore and charcoal in a forge or furnace having a forced draft. 4. The iron produced under these conditions usually contained about 3 percent of slag particles and 0.1 percent of other impurities. Occasionally this technique of iron`making produced, by accident, a true steel rather than wrought iron. 5. Ironworkers learned to make steel by heating wrought iron and charcoal in clay boxes for a period of several days. By this process the iron absorbed enough carbon to become a true steel.
History of Iron making :

## Slide 4
Iron ore
Pellet
Limestone
Coke
Sintered
ore
Blast furnace
(BF)
Hot metal
Basic oxygen furnace
(BOF)
Scrap
Iron making
Electric arc furnace
(EAF)
Steel making
Continuous casting
Hot
direct
rolling
(HDR)
Billet
Bloom
Slab
Reheating furnace
Steel casting
Rolling
Seamless pipe mill
Seamless pip
Welded pipe mill
Welded pipe
Butt welded pipe
Cold rolling tandem mill
Cold rolled coil
and sheet
(also for plating)
Hot strip mill
Hot rolled coil
and sheet
Main products
Plate mill
Plate
Wire rod mill
Wire rod
Section mill
Bar
Shape
Sheet pile
Rail
General flow diagram of Iron – Steel making process :

## Slide 5
Stock House
Hot Blast Stoves
Gas Cleaning
Scrubber
Bell Less Top
Blower
Combustion Air
Slag, Hot Metal
Gasholder
Enrichment Gas
Combustion Gas
Sinter
Coke
Different section of blast furnace plant :

## Slide 6
Hearth Refractories
Tuyeres
Bustle Main
Refractory Lining
Throat Armour
Top Bins
Top Gas Mains
Above Burden Probe
Temperature Probe
Sub Burden Probe
Operation Over-View :
The Blast Furnace Process
1. The Iron Ore, Coke and Limestone, (the Charge), is conveyed to the top of the Furnace. 2. The Charge is stored in Bells until the timing is right for the charge to be dropped into the Furnace. 3. Hot air is then blown through pipes called Tuyeres, to fire the mixture. 4. The Coke burns to increase the temperature in the Furnace. 5. The Limestone attracts the impurities in the Iron Ore and forms Slag. This Slag is lighter than the molten Iron and so floats on top of it. 6. As the Furnace fills, the molten Iron is Tapped off. The Slag is also tapped off at regular intervals. Most Iron is taken straight from the Blast Furnace to the Steel Mill, but some is poured into buckets called Pigs. This Iron is called Pig Iron and is used to make Cast Iron.

## Slide 7
Hematite Fe2O3
Magnetite Fe3O4
Limonite Fe2O3. xH2O
Siderite FeCO3
Iron
Ore
Fe content : 20 - 70%
SiO2
Al2O3
CaO
MgO
S
- unwanted, less than 0,15%
P, As
Flux
Lime, dolomite CaMgCO3 , CaO
Coke
Metallurgical coke
Raw Material for Blast Furnace :
Hot Air / Gas
Coke oven / Blast Furnace Gas / Hot Air

## Slide 8
Schematic diagram of B/F :

## Slide 9
Main reactions in blast furnace :

## Slide 10
Avg. Input for 1 T Iron Production with Chemistry
Coke
Hot Gases
1t Pig Iron
Flux
Ore
0.35 – 0.6t
0.4t
2t
3.5 t Gas
Fe | C | Si | Mn | P | S
90-95% | 3.0-4.3% | 0.5-3.0% | 0.5-3.0% | 0.05-2% | do 0.1%
Chemical composition

## Slide 11
Pig Iron is being casted to
ingot
TORPEDO LADLE
Product of Blast Furnace

## Slide 12
Other Product of Blast Furnace
Slags
SiO2 | CaO | Al2O3 | MgO, MnO, FeO, CaS, MnS, P2O5, BaS, atd.
26-40% | 36-48% | 10-20% | negligible
Chemical composition
Stock gas
Chemical composition
CO2 | CO | H2 | CH4 | N2
8-14% | 23-32% | 1-4% | 0,2-0,4% | 55-60%

## Slide 13
History of Steel making :

## Slide 14
Introduction of Steel making furnaces :
- There are three core root for production of steel.
Open Hearth Process
Basic Oxygen Process
Electric Arc Furnace

## Slide 15
Open Hearth Process :
The Converter
Melted high carbon iron (pig iron) + bottom injected air
Fast reaction:
[Fe-C] + {O2 } → [Fe] + {CO }
Minor reaction :
[Fe] + {O2 } → (FeO)
Liquid steel product
SiO2 lining (acidic)
Melted iron (pig iron + scrap) + hot air + flue gas
+ magnesite lining + CaO powder

## Slide 17
Basic Oxygen Process:
[Fe-C] + {O2 } → [Fe] + {CO } [Fe-P-S-Si] + {O2 } + <CaO> → [Fe] + (P,S,Si in slag)
Liquid pig iron from blast furnace (higher content of C, Si, P, S,…)
Steel scrap (variable composition - also Cu, Zn, Pb, Cd,…)
Iron from direct reduction process (bloom, sponge, briquettes – quite pure Fe)
30-40%
60-70%
< 10%

## Slide 18: BOS Steel batch 200 000 kg O2 : 500 normal m3/min 20 min Superficial velocity 1.5 m/s 250 vvm Gas power input 60 kW/m3 (or 8 W/kg) Mixing time 10-100 s Whole cycle 50 min
Ladle
Steel
Scrap
Slag
Oxygen tuyere
Oxygen Lance
Liquid steel
Operation over-view of Basic Oxygen Process:

## Slide 19
Electric Arc Furnace :

## Slide 23
Ladle Treatment :

## Slide 24
Ladle / Tundish Treatment :

## Slide 25
Continues Casting of Steel:

## Slide 26
Continues Casting of Steel:

## Slide 27
Hot rolling of steel:

## Slide 28
Hot rolling Product :

## Slide 29
Thank You….for attention
Any Questions….??