BREWER COTE® ACRYLIC COAT

BREWER COTE OF ARIZONA 
5226 W. MISSOURI AVE 
GLENDALE, AZ 85301 
(623)931-3728    (888)931-3728

sales@brewercoteaz.com 
www.brewercoteaz.com

DESCRIPTION

This highly milled emulsion uses the benefits of cationic binders and polymers, produces a superior sealer. 
Acrylic Coat attaches and seals the asphalt sub-strait and is highly resistant to UV, water and fuel 
Acrylic Coat is a blend of select mineral fillers, plasterers and asphaltenes in a stable P.G. Grade asphalt

ADVANTAGES

  - Protects surface from Ultra violet rays

  - Binds aggregate into surface, reduces raveling

  - Easy to apply

  - Fast Drying

  - Prevents water damage

  - Resists cracking and chipping better than other sealers

  - Environmentally safe

  - Oil and fuel resistant

  - Can be customized with aggregate Loading

  - Flexible coating

Characteristics

Method of Application: Brush, Squeegee or Conventional Oil spreading equipment

Color: Satin Black

Weather Limitations: For best results, do not apply on rainy, Foggy or extremely Humid days 
or when temperature is expected to drop below 50° F during the next 6 hrs

Drying Time: 2 Hour Maximum

Clean Up: Water Soluble tar and asphalt remover

Packaged: 5 Gallon Pail (49Ibs), 55 Gallon Drum (520Ibs), Bulk 7.

|  |  |  | Application Rate |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dilution Rate |  |  | Quantity of Emulsions |  |  |  | Quantity of Aggregate |  |
|  |  |  |  | gal/vd" (I/m2) |  |  | lb/vd" (kg/rn" |  |
| 1:1 |  |  |  | 0.10 - 0.15 |  |  |  | 0.20 - 0.50 |
|  |  |  |  | (0.45 - 0.68) |  |  | (0.11 - 0.27) |  |
| 2:1 |  |  |  | 0.08 - 0.15 |  |  |  | 0.20 - 0.50 |
|  |  |  |  | (0.36 - 0.54) |  |  | (0.11 - 0.27) |  |
|  |  | One to One Dilution Emulsion Properties |  |  |  |  |  |  |
| Properties |  |  |  | Specifications |  |  |  | Limits |
| In Ready to Apply form, one part concentrate to one part Water By Volume |  |  |  |  |  |  |  |  |
| Saybolt Furol Viscosity at |  |  |  | ASTM D244 |  |  | 10 - 50 Seconds |  |
| 77"F (25°C) |  |  |  |  |  |  |  |  |
| Residue by Distillation or |  |  |  | ASTM D244 |  |  | 28.5 Minimum |  |
| Evaporation |  |  |  |  |  |  |  |  |
| Pump Stability' |  |  |  |  |  |  |  | Pass |
|  | Emulsion Residue by Distillation or Evaporation Tests |  |  |  |  |  |  |  |
| Properties |  |  |  | Specifications |  |  |  | Limits |
| Viscosity at 275°F (135°C) |  |  |  | ASTM D4402 |  |  | 1750 cts Maximum |  |
| Solubility in 1,1,1 |  |  |  | ASTM D2042 |  |  | 97.5 Minimum |  |
| Trichloroethlene |  |  |  |  |  |  |  |  |
| Penetration |  |  |  | ASTM D5 |  |  | 50 dmm Minimum |  |
| Asphaltenes |  |  |  | ASTM D2007 |  |  | 15 Minimum |  |
| Saturates |  |  |  | ASTM D2007 |  |  | 15 Minimum |  |
| Polar Compounds |  |  |  | ASTM D2007 |  |  | 25 Minimum |  |
| Aromatics |  |  |  | ASTM D2007 |  |  | 15 Minimum |  |
|  |  | Aggregate Material Gradation Requirements |  |  |  |  |  |  |
|  | Sieve Designation |  |  |  | Percentages of Weight |  |  |  |
|  | Square Openings |  |  |  | Retained Sieves |  |  |  |
|  |  | NO.8 (2.38mm) |  |  | 0 |  |  |  |
|  | No. 16 (1.19mm) |  |  |  | 0-8 |  |  |  |
|  | No. 20 (0.84mm) |  |  |  | 0-28 |  |  |  |
|  | No. 30 (0.60mm) |  |  |  | 20-50 |  |  |  |
|  | No. 40 (0.42mm) |  |  |  | 10-55 |  |  |  |
|  | No. 50 (0.30mm) |  |  |  | 0-30 |  |  |  |
|  | No. 70 (0.21mm) |  |  |  | 0-5 |  |  |  |
|  | No. 100 (0.15mm) |  |  |  | 0-2 |  |  |  |
|  | No. 200 (0.07mm) |  |  |  | 0-2 |  |  |  |