5226 West Missouri Avenue    Glendale, Arizona  85301

Office (623) 931-3728	toll free (888) 931-3728	facsimile (623) 842-0714

www.brewercoteaz.com

FlexSet Elastic Concrete

FlexSet combines polymers with a specially-treated aggregate to create a rapid-setting, easy-to-apply, long-lasting and durable concrete repair. Repairs can be done in minutes, using only 4 simple steps. Originally, developed for the U.S. Air Force as a rapid runway repair material, FlexSet has become an inexpensive alternative to traditional concrete restoration procedures. This innovative, patent pending process provides a modern solution to an age old problem. FlexSet repairs are guaranteed to perform

FlexSet ™ Elastic Concrete

FlexSet Elastic Concrete is a flexible concrete comprised of elastic cement and coated silica quartz mix.

FlexSet Elastic Concrete is supplied in 5 gallon pails comprised of: 43 lbs Polymer Coated Silica Quartz, 1/2 gallon of Elastic Cement A, 1/2 gallon of Elastic Cement B, and 10 lbs of Polymer Coated Topping Sand.

Packaging & Coverage: Each 5 gallon container of FlexSet Elastic Cement will fill .4 cubic feet (691 cubic inches). 125 lbs of Elastic Concrete will fill one cubic foot. The coverage rate is:

Thickness	Coverage /Sq Ft		Thickness	Coverage / Sq Ft

1/8"		         38.4		     5/8"		         7.7

1/4"		         19.2		     3/4"		         6.4

3/8"		         12.8		     7/8"		         5.5

1/2"		          9.6		       1"		         4.8

Safety: FlexSet Elastic Concrete is not a significant skin or eye irritant Nevertheless, Skin or eye contact may lead to sensitization. Appropriate protection is necessary. Gloves and safety glasses are required for handling FlexSet. Wash hands before eating, drinking, and smoking after handling material.

Surface Preparation: Remove loose & unsound material. Sand Blast or shot blast contaminated surfaces. Clean & blow out cracks with dry compressed air. Dry wet surfaces. Moist surfaces create a weak bond and foaming. Caution: Use opened containers right away to avoid moisture contamination.

Mixing: Add 1/2 gallon of "A" to coated sand mix. Mix thoroughly with heavy duty mixer (about 2 minutes). Next, add 1/2 gallon of "B" and mix thoroughly (1 minute). Blend is pourable, working time is approximately 15 minutes at 75 degrees.

Installation : Squeegee, spread, gauge-rake or trowel. Broadcast surface with topping sand. For deep repairs, FlexSet can be placed in lifts topping each lift with aggregate. Install at temperatures between - 25 deg C to 40 deg C (- 14 deg F to 104 deg F).

Cure: Cure for 1 hour minimum at 75 deg F before subjecting to traffic. Cold temperatures slow cure. At 55 Deg F, 4 hour cure is needed for open traffic. Cold weather cure is accelerated by maintaining repair kits warm prior to application.

Shelf Life: FlexSet Elastic Concrete shelf life is 1 year when stored indoors, unopened under cool & dry conditions. Avoid wet storage conditions. Dispose empty containers in accordance with all local , state, and federal regulations.

First Aid: If Inhaled, remove to fresh air, if not breathing, give artificial respiration, preferably mouth to mouth. If breathing is difficult give oxygen and call physician. Skin Contact: Wash skin with soap and water. Remove contaminated clothing. Eye Contact: Flush with water for at least 15 minutes and call physician.

Spill or Leakage: In case of a liquid spill of unmixed materials A & B absorb spilled material with sawdust or other absorbent Sweep into container and neutralize with decontamination solution (95% water, 5% ammonia & 2% detergent). Store open containers outdoors for at least 24 hours. Dispose of neutralized waste in accordance with local, state and federal government environmental regulations.