5226 W. Missouri Avenue

Glendale, Arizona 85301

1-888-931-3728

Rhino Hide is a blend of emulsified asphalt, clean aggregate, modifiers, fiber, rubber, and drying agents. Designed especially for heavy duty repairs of alligatoring and skin patching, along with serious crack repair. Rhino Hide can be used to build up depressions, fill expansion joints and wide cracks or any other job requiring a trowel grade, heavy duty, fast drying modified asphalt.

J.B. INDUSTRIAL			OAHU SEALCOATING		SUN SEALER			NEAL & SONS

BILLINGS, MONTANA		OAHU, HAWAII			RENO, NEVADA	      		LAS VEGAS, NV

PHONE (406) 245-3128		PHONE (808) 682-0975		PHONE (775) 359-2337		PHONE (702) 459-2992

FAX (406) 245-8834		FAX (808) 682-1406		FAX (775) 358-7072		FAX (702) 643-2796

BREWER COTE ®

RHINO HIDE

APPLICATION INSTRUCTIONS

APPLICATION:		 Pour/trowel into alligatored areas and work with

squeegee, feather in edges.

FILLING CRACKS: 		Fill cracks, scrape excess from surface before setting

(Use V-shape squeegee).

FILLING BIRD BATHS: 	Fill with lifts of 1” depth maximum, allow to harden

before applying seal coating.

*A second coat can be applied after the 1st coat dry’s

to blend better with the substrait.

Cement maybe blended with Rhino Hide for 	          Clean area of all dirt, dust, and loose

quicker set up.    				          material. Surface must be dry and clean

COVERAGE:			5 Gallons covers:  8 SQ.FT. @ 1” thick

96 LF @ 1” x 1”

DRYING TIME:		½” Lifts; 4 hours, 1” Lift; 6-8 hours, based on 77º F,

50% Hum. Test for trafficability before opening.

If traffic must be opened, broadcast with sand.

WEATHER CONDITIONS:  	For best results, do not use when rain is in the

forecast and temperature is not expected to drop

below 55 degrees F. Rhino Hide is no substitute for

properly replaced asphalt, Rhino Hide will prolong

the life of the deteriorated asphalt.

COLOR:			Black							Prime area with diluted tack oil

(1 to 1, allow to dry)

CLEAN UP:			Paint thinner and Biodegradable solvents.

PACKING:			Five and Fifty five gallon drums.

Rental tank available for bulk.

NOTE:				Keep from freezing and direct sunlight or when

temperature exceeds 100 F.

Pour/Trowel into distressed area, work with squeegee feather edge.