AP Lazer

CerMark Ultra on stainless steel cups

Thinned with denatured alcohol and brushed on with a foam brush.

100 watt SN4836, Scan gap of .003 but diameter might have been slightly off.

Power 45 Speed 20 came out the best on this unit.



