Directions for Application:
Clean chain and rinse with isopropyl alcohol for best bond.
Apply Smoothe Lube™ directly to rollers while turning cranks slowly to prevent fly-off.
Use brush provided to work product into rollers and between side plates while turning cranks.
For Hot wax-dipped chains: one coat is all that is usually needed as an easy re-application until next cleaning and/or used as a supplement for smoother/quieter performance.
For chains that are freshly cleaned: apply one coat as directed or Start with Lübenschlidən™ as the first coat. Wait 20 mins or until dry then add a second coat to ensure all areas between rollers and side plates are covered. Skillfully lay off lube with the brush to leave a light film on contact surfaces for superquiet performance. May be polished clean when dry with a toothbrush if desired but may not be as quiet while riding. Re-Lube after riding only requires 1 application of Smoothe Lube
NOTE: a new chain requires a 'break in' period and simultaneously establish the wax and particles into the chain. This can take up to 50 miles to have the burnishing effect our products were designed to do. Once established, our product becomes more quite over time.
Re-application of Smoothe Lube:
Whether your chain is cleaned from all other chain lubes or still has factory grease installed, you can reapply Smoothe Lube easily.
For Quick Cleaning- clean your chain while you wash your bike, with water and any other product you may already use. Removing as much dirt and dust as possible. A small stiff brush or toothbrush will be adequate. Smoothe lube is designed to clean itself upon each application and will dislodge much of the dust and dirt.
Thorough Cleaning- Isopropyl Alcohol is all needed to dissolve Smoothe Lube at this point, with the chain on the bike or chain removed and soaked in a jar.
NOTE: product is designed to clean itself and eliminate the time consuming cleaning once Smoothe Lube is established on the chain and still provide excellent performance
Clean up:	While product is sill wet it can be cleaned with water. When dry or for product removal, Isopropyl alcohol is all that is needed for Smoothe Lube.
Chain cleaning tips:	1st application-Soaking chain in a jar of solvent will remove most of the existing lube, factory lube, other wax lubes, ect. Simple Green is a good biodegradable solvent to use. This method is best to completely remove product if desired
Once you have thoroughly cleaned/degreased your chain, a quick alcohol rinse will ensure wax bonding to the chain surfaces, as well as help neutralize any acids from the degreasers or solvents used in cleaning.
Application Videos: Currently on instagram @amtberproducts and YouTube at aMTBerProducts YouTube link- https://youtu.be/sCR-zXzTvhU
Thank You for trying Smoothe Lube and Lubenschliden! Give us a call or email if you have any questions: 818-835-0697 info@aMTBer.com