- SECTION 09 72 23 – CEMENTITIOUS COATING

- PART 1 GENERAL

  - RELATED DOCUMENTS

- General provisions of the Contract, including General and Supplementary Conditions, Drawings, and Division 01 Specifications, apply to this Section.

- 1.03	RELATED DIVISIONS

- Division 03- Concrete

- Division 07- Thermal and Moisture Protection

- Division 22- Plumbing

- 1.04      SYSTEM DESCRIPTION

- Versicrete Smooth is a 1/8” thick (nominal) four-component polymeric-cement flooring system consisting of a primer, MC medium, MC Bond, MC Fine MC SealCoat and MC TopCoat..

- 1.05	SUBMITTALS

- General: Submit the following in accordance with Conditions of Contract and Division 1 Specification Sections.

- Product Data: Submit manufacturer's technical data, application instructions, and general recommendations for the flooring specified herein.

- Samples for initial selection purposes in the form of manufacturer's color charts showing the

full range of colors and finishes available.

- Maintenance Instructions: Submit manufacturer's written instructions for recommended maintenance practices.

- 1.06	QUALITY ASSURANCE

A.	Installer Qualifications: Engage an experienced Installer or applicator who specializes in installing microcement overlays similar to that required for this project and who is acceptable to the manufacturer of primary materials.

B.	Single-Source Responsibility: Obtain flooring materials, including primers, mortars, seal coats, and topcoats from a single manufacturer.

C.	Qualified Materials: Request for material approvals for any products other than the specified products must be submitted to the architect two weeks before the bid, including complete application specification, physical and aesthetic characteristics. Any request after this date will not be accepted. Failure of performance requires immediate removal and replacement of unapproved substituted material with those specified initially at no cost to the owner, architect, construction manager, or general contractor.

- 1.07      DELIVERY, STORAGE AND HANDLING

A.	Deliver materials in original packages and containers with seals unbroken and bearing manufacturer's labels containing the brand name and directions for storage and mixing with other components.

B.	Store materials to comply with the manufacturer's directions to prevent deterioration from moisture, heat, cold, direct sunlight, or other detrimental effects.

- 1.08	PROJECT CONDITIONS

A.	Environmental Conditions: Comply with flooring manufacturer's directions for maintenance of ambient and substrate temperature, moisture, humidity, ventilation, and other conditions required to execute and protect work.

B.	Lighting: Permanent lighting will be in place and working before installing flooring.

- PART 2.00 - PRODUCTS

- 2.01	MATERIALS

- Microcement flooring system shall be Versicrete Smooth is a five-component cementitious polymeric product.as manufactured by Versicrete, LLC Wallington, New Jersey.

- 2.02	PHYSICAL CHARACTERISTICS

A.	Colors:  As selected by Architect from manufacturer's standard colors.

B.	Physical Properties:

Provide a flooring system that meets or exceeds the listed minimum physical property requirements when tested according to the referenced standard test method in parentheses.

- Compressive Strength (ASTM C579)	13,053 psi.

Flexural Strength (ASTM C580).	7,2511 psi.

Hardness (ASTM D2240)	80 Durometer "D"

Impact Resistance (ASTM D4226)	>132 in. lbs.

Flammability (ASTM D635)	Class A1

Water Absorption (ASTM C413)………………………………0%

Percent Solids…………………………………………………..43%

Cure Rate (@77°F/25°C).………………………………………12 hours Tack Free

24 hours normal operations

- 2.03	SUPPLEMENTAL MATERIALS

A.	Waterproofing Membrane: Type recommended or produced by the manufacturer of the flooring system for the type of service and floor condition indicated.

- PART 3.00 - EXECUTION

- 3.01     INSPECTION

- Examine the areas and conditions where the urethane coating is to be installed and notify the Architect of conditions detrimental to the proper and timely completion of the work.  Do not proceed with the work until the Contractor has corrected unsatisfactory conditions in a manner acceptable to the Architect.

B.    Test for moisture vapor transmission. Notify Architect immediately if moisture vapor transmission exceeds manufacturers’ recommended levels.

- 3.02	PREPARATION

A.	Substrate: Perform preparation and cleaning procedures according to the flooring manufacturer's instructions for substrate conditions involved, and as specified. Provide a clean, dry, and neutral substrate for flooring application.

B.	Concrete Surfaces: Mechanically abrade the substrate to remove enough material to provide a concrete surface profile of CSP-3 or CSP-4. Surface shall be free of laitance, glaze, efflorescence,

and any bond-inhibiting curing compounds or form release agents.  Repair damaged and deteriorated concrete to a condition acceptable to successfully receive the flooring system.

C.	Materials: Mix resin hardener and aggregate when required and prepare materials according to flooring system manufacturer's instructions.

- 3.03	APPLICATION

A.	General: Apply each component of the flooring system according to the manufacturer's directions to produce a uniform, monolithic flooring surface of thickness indicated.

- Primer: Mix and apply MC Prime (when necessary) over properly prepared substrate at specified spread rate.

- Mix and apply MC Medium over primed substrate. Allow to cure.

- Apply MC Bond to MC Medium. Allow to cure

- Mix and apply MC Medium.

- Mix and apply MC Fine to dampened MC Medium using Smooth finish technique,

- Mix and apply MC SealCoat. Allow to cure

- Mix and apply MC TopCoat within eighteen (18) hours.

- 3.04	CURING, PROTECTION AND CLEANING

- Cure the flooring materials according to the manufacturer's directions.

- Prevent contamination during application stages and before completing the curing process.

Close the area of application for a minimum of 24 hours.

- Protect the finished floor.

- Clean with manufacturer recommended cleaner.

- END OF SECTION