| Part #31101 REFERENCE GUIDE V2.43 |  | ## IT TODAY, ## PUT IT TO WORK TOMORROW! |
| --- | --- | --- |
| SMALL INDUSTRIAL KIT (w/ hardener) CONTENTS (1) 1 Gallon Dakota Prep (1) 1 Gallon Dakota Shine (1) 8 fl oz Catalyst Hardener (4) Disposable Measuring Cups (1) Stir Stick (6) Scrub Pads (heavy duty) EQUIPMENT NEEDED - Paint Gun - 1.4mm Tip - Conventional, Gravity Feed recommended - Regulator - Set to ~60 psi - Water/Oil Trap - Air Hose - Solvent (for cleanup) - OEM Exact Match Paint - Optional Paint Touch-Up - Respirator & Gloves (recommended) - Clean Towel - Rags - Wash Bucket - Water Hose - Pressure Washer NEED ACCESS TO - Wash Bay - Water Hose - Pressure Washer - Air Compressor - Well-ventilated area for application, if available | STEP 1 ¦ CLEAN & DEGREASE. STEP 2 ¦ DAKOTA PREP; Similar to the process of wet sanding by hand to lift and break up oxidation. #### Mix ~ 8oz Dakota Prep with ~ 1gal water and soak the scrub pads in the bucket #### Scrub the oxidized surface with a wet, saturated pad and Dakota Prep from the bucket, avoid excessive pressure, rinse often (similar to wet sanding by hand) #### Focus on areas with greatest eye appeal, including wheels, hoods, panels #### Keep pad wet and rinse in the bucket of Dakota Prep often to avoid scratching #### If Dakota Prep dries on the surface, repeat this step on that area #### Rinse the entire unit with fresh water and allow to dry completely. STEP 3 ¦ DAKOTA SHINE; Fix Faded Paint. #### If necessary, areas of missing paint can be touched up at this point – Use only OEM Exact Match Paint and feather out the coverage (optional) #### Prepare equipment as directed then add the equivalent of 2oz Catalyst Hardener to 1qt Dakota Shine and mix before transferring to paint gun cup #### Apply one thin layer of Dakota Shine using an even spray pattern – Split tracks on every pass and keep the paint gun perpendicular to the surface #### MORE IS NOT BETTER – focus on thin, light and uniform passes #### Do not coat the surface as you would with paint #### Use cardboard or mask to prevent unwanted overspray #### Overspray on glass can be cleaned with solvent – avoid spraying plexiglass #### Results should be seen almost immediately #### There is about a 20-minute window to correct any mistakes once started #### If a spot was missed, feather out any overlap in one thin, light uniform pass #### Beyond 20-minutes, spot fixes will not blend #### Once finished, let unit sit for as long as possible, keep away from rain and dust #### Drying and recommended exposure times listed below. #### STEP 4 ¦ CLEANUP. #### Add 1 - 2oz of Solvent to the spray gun cup and swirl #### While still connected to air, trigger the gun in a safe direction to clear tip #### Any overspray on glass can be wiped with Solvent and a Rag. |
| #### We suggest allowing a minimum of - 1 to 4 hours until the surface is dry (avoid dust) - 2 hours before exposure to harsh outside elements - 12 hours before exposure to a work environment - 1 week before exposure to aggressive cleaning - 4+ weeks before reapplying Dakota Shine |  | #### For more in depth instructions and additional tips, scan below Support@DakotaShine.com www.DakotaShine.com Help Line: 888-996-7801 |