Crystal Paints 
5 Curban St, Underwood QLD 4119
PH: 07 3341 3566

Silvercoat

One Coat Wonder – Roof & Metal Paint

High-Quality Silver Coat with Exceptional Coverage Strength

- Suitable for most metal surfaces, including roofs, structural steel, and more

- Easy application by brush, roller, or spray

- If spraying, you may need to thin with mineral turps to suit your spray gun

- Recoat time: 3 to 8 hours, depending on conditions

Surface Preparation:

- Raw steel must be primed with Grey Oxide Primer

- Bare timber requires a suitable primer or undercoat

- Always apply a test patch to the prepared surface before full application

Coverage:
8–16 square metres per litre (depending on surface and application method)

Thinning & Clean-Up:
Use mineral turps only
Do not mix with other paints

Available Sizes:

IF YOU ARE UNSURE ABOUT ANYTHING TO DO WITH THIS PRODUCT DO NOT USE IT AND CONTACT YOUR CRYSTAL STOCKIST OR THE FACTORY DIRECT