**Crystal Paints
5 Curban St, Underwood QLD 4119
PH: 07 3341 3566**

**Tile, Laminate & Melamine**

* **Multiple Application Methods:** Brush, roll, or spray – Crystal Paints Tile, Laminate & Melamine Paint accommodates your preferred application technique, providing flexibility for various surfaces, including benchtops, doors, walls, and more.

**Preparation:**

* **For Tiles:** Sand tiles with 240 – 320 grit sandpaper, ensuring a thorough cleaning for a perfect surface. Eliminate any shiny tile surfaces. For floors, incorporate anti-slip grit between coats for added safety.
* **For Laminate & Melamine:** Sand with 240 – 320 grit sandpaper and clean meticulously. Non-experienced painters can achieve the best results using a fine bristle brush or a short nap roller like mohair. If spraying, thin the paint with mineral turps for a flawless finish.

**Drying and Recoat:**

* Crystal Paints Tile, Laminate & Melamine Paint dries in 2-4 hours, with a recoat time of 2-4 hours depending on weather conditions. for the best results, it is recommended to recoat after 12 to 24 hours to achieve a harder and stronger finish. Full curing time is at least 1-3 weeks.

**Application Tips:**

* **Proper Mixing:** Stir the paint well and check for settling at the bottom of the can before applying.
* **Coverage:** 1 litre can cover up to 12 square meters on tiles, with potential for more depending on tile grout.

**Clean Up:** Use Mineral turpentine for easy and effective cleanup. Don't use any cleaning products that leave a residue.

**Cautions and Recommendations:**

* **Temperature Consideration:** Avoid painting in temperatures less than 12 degrees Celsius.

**Extra Tips for Excellence:**

* **Enhanced Hardness:** Leaving a day between coats accelerates hardness. Lightly sand with 240 grit before each coat for a smooth, glossy finish.

IF YOU ARE UNSURE ABOUT ANYTHING TO DO WITH THIS PRODUCT DO NOT USE IT AND CONTACT YOUR CRYSTAL STOCKIST OR THE FACTORY DIRECT

